| TempSmart Athermal Package Zirconium Tungstate NTE Ceramic |  |
| --- | --- |
| Features Negative thermal expansion characteristics Compensate for FBG fiber thermal effect Very wide operating temperature range and linear expansion Compact package | Formula | ZrW2O8 |
|  | Crystal symmetry | Isotropic |
|  | Coefficient of Thermal Expansion (CTE) | –10*10-6/K |
|  | Operating temperature range | 0.3K ~ 1050K |
|  | CTE tunable range | -9*10-6/K ~ -10*10-6/K |
| ZrW2O8 Crystal Structure |
| Thermal Expansion Characteristics: |